## Slide 1
Problem: Erosion is a process of essential implications for the pump industry for financial losses
Approach: Evaluate analytical models and transfer these into a numerical simulation tool; erosion onset can pre-selecting appropriate materials
Results: Erosion can be simulated analytically and numerically
The FE-Model forecasts incubation time + applicable operation ranges
Outlook: Extended prediction abilities, especially erosion rates for material qualification
Dr. A. Krebs: Simulation of Erosion Begin for MMCs
Dr.-Ing. A. Krebs
Chart: Particle Velocity v [m/s]
| 20 | 30 | 40 | 50
Inkubationsphase Kobalt | 30 | 13 | 7 | 4
Chart: Particle Hits
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29
v = 50 m/s, α = 90° | 0 | 0 | 0 | 0 | 1.4607e-05 | 2.3708e-05 | 3.3371e-05 | 4.5056e-05 | 4.7416e-05 | 5.6854e-05 | 5.9326e-05 | 7.6292e-05 | 9.0562e-05 | 9.0562e-05 | 9.1461e-05 | 0.00010281 | 0.00011067 | 0.00011539 | 0.00012584 | 0.00014517 | 0.00014955 | 0.00016494 | 0.00017281 | 0.0001736 | 0.0001736 | 0.00017573 | 0.00018933 | 0.00019719 | 0.00020584 | 0.00020854
v = 40 m/s, α = 90° | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.5506e-05 | 2.3258e-05 | 3.0112e-05 | 3.8315e-05 | 4.3371e-05 | 4.5281e-05 | 4.5281e-05 | 5.0449e-05 | 5.7079e-05 | 5.764e-05 | 5.764e-05 | 6.2697e-05 | 7.9775e-05 | 8.6404e-05 | 9.0787e-05 | 9.1685e-05 | 9.9213e-05 | 0.00010461 | 0.0001118 | 0.00011539 | 0.00011607 | 0.00011652 | 0.00012528
v = 30 m/s, α = 90° | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4.7191e-06 | 1.3596e-05 | 1.6854e-05 | 2.1798e-05 | 2.3708e-05 | 2.9888e-05 | 3.2921e-05 | 3.8876e-05 | 4.1573e-05 | 4.2022e-05 | 4.4494e-05 | 4.5393e-05 | 4.6517e-05 | 5.0562e-05 | 5.0562e-05 | 5.3596e-05 | 5.6742e-05
v = 20 m/s, α = 90° | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Operation Range
Incubation Time vs. Part. Velocity, Hit-#) Incubation Time = f(Particle Velocity); Operation Ranges
no-go area